# MATERIAL EXTRACTION REPORT

Generated: 2/2/2026, 5:05:34 PM

Total Materials: 41

Source: Audco India Ltd Technical Bulletin No: 1

## EXTRACTED MATERIALS

Material 1: ASTM A182 Grade F1

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - Carbon-Molybdenum |
| Grade | F1 |
| Designation | UNS K12822 |
| CHEMICAL COMPOSITION |  |
| Composition | C-Mo Steel (0.5% Mo) |
| Chromium (Cr) | Not specified |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.44-0.65% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.28% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 485 MPa min (70 ksi) |
| Yield Strength | 275 MPa min (40 ksi) |
| Elongation | 20% min |
| Hardness | 143-192 HBW |
| HEAT TREATMENT |  |
| Temperature | Anneal at 1550°F (900°C) |
| Soaking Time | Per thickness |
| Cooling Method | Furnace cool |
| WELDING PARAMETERS |  |
| Weldability | Good with preheat |
| Electrode Type | E 7018-A 1 |
| Preheating | 200-400°F (95-205°C) |
| Interpass Temperature | 400°F (205°C) max |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1150°F (620°C) minimum |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Moderate |
| Applications | Moderate temperature service up to 482°C (900°F); Pressure vessels; Piping systems |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Low |
| Structure | Ferritic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 2: ASTM A182 Grade F5

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - 5Cr-0.5Mo |
| Grade | F5 |
| Designation | UNS K41545 |
| CHEMICAL COMPOSITION |  |
| Composition | 5% Cr, 0.5% Mo |
| Chromium (Cr) | 4.0-6.0% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.44-0.65% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.15% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 485 MPa min (70 ksi) |
| Yield Strength | 275 MPa min (40 ksi) |
| Elongation | 20% min |
| Hardness | 143-217 HBW |
| HEAT TREATMENT |  |
| Temperature | Normalize & Temper at 1150°F (620°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | E 502-15 or 16 |
| Preheating | 400-700°F (205-370°C) |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1250°F (675°C) minimum |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - High temperature |
| Applications | High-temperature service up to 593°C; Hydrogen service; Refinery equipment |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Medium |
| Structure | Ferritic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 3: ASTM A182 Grade F9

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - 9Cr-1Mo |
| Grade | F9 |
| Designation | UNS K90901 |
| CHEMICAL COMPOSITION |  |
| Composition | 9% Cr, 1% Mo |
| Chromium (Cr) | 8.00-10.00% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.90-1.10% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.15% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 485 MPa min (70 ksi) |
| Yield Strength | 275 MPa min (40 ksi) |
| Elongation | 20% min |
| Hardness | 187-248 HBW |
| HEAT TREATMENT |  |
| Temperature | Normalize & Temper at 1250°F (675°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | E 505-15 or 16 |
| Preheating | 400-700°F (205-370°C) |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1250°F (675°C) minimum |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Steam oxidation |
| Applications | High-temperature service up to 593°C; Steam power generation; Petrochemical industry |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Medium |
| Structure | Ferritic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 4: ASTM A182 Grade F11 Class 1

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - 1.25Cr-0.5Mo |
| Grade | F11 |
| Designation | UNS K11597 |
| CHEMICAL COMPOSITION |  |
| Composition | 1.25% Cr, 0.5% Mo (Low Carbon) |
| Chromium (Cr) | 1.00-1.50% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.44-0.65% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.05-0.15% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 415 MPa min (60 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 20% min |
| Hardness | 121-174 HBW |
| HEAT TREATMENT |  |
| Temperature | Normalize & Temper at 1150°F (620°C) minimum |
| Soaking Time | Per thickness |
| Cooling Method | Air cool after normalizing |
| WELDING PARAMETERS |  |
| Weldability | Good - Preheat and PWHT required |
| Electrode Type | E 8018-B 2 |
| Preheating | 300-600°F (150-315°C) |
| Interpass Temperature | 600°F (315°C) max |
| Heat Input | Controlled |
| Post-weld Heat Treatment | 1150°F (620°C) minimum |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Moderate - High temperature oxidation resistance |
| Applications | High-temperature piping up to 593°C (1100°F); Steam systems and headers; Pressure vessels; Refinery and petrochemical equipment; Elevated temperature service |
| Standards | ASTM A182, ASME SA-182, ASTM A370 |
| Cost Level | Low to Medium |
| Structure | Ferritic + Pearlite |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 5: ASTM A182 Grade F12

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - 1Cr-0.5Mo |
| Grade | F12 |
| Designation | UNS K11572 |
| CHEMICAL COMPOSITION |  |
| Composition | 1% Cr, 0.5% Mo |
| Chromium (Cr) | 0.80-1.25% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.44-0.65% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.05-0.15% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 415 MPa min (60 ksi) |
| Yield Strength | 220 MPa min (32 ksi) |
| Elongation | 20% min |
| Hardness | 156-207 HBW |
| HEAT TREATMENT |  |
| Temperature | Normalize & Temper at 1150°F (620°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | E 8018-B 2 |
| Preheating | 300-600°F (150-315°C) |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1150°F (620°C) minimum |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Moderate |
| Applications | High-temperature piping; Pressure vessels; Petroleum refining |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Low-Medium |
| Structure | Ferritic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 6: ASTM A182 Grade F22 Class 1

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - 2.25Cr-1Mo |
| Grade | F22 |
| Designation | UNS K21590 |
| CHEMICAL COMPOSITION |  |
| Composition | 2.25% Cr, 1% Mo |
| Chromium (Cr) | 2.00-2.50% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.87-1.13% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.05-0.15% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 415 MPa min (60 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 20% min |
| Hardness | 170 HBW max |
| HEAT TREATMENT |  |
| Temperature | Normalize & Temper at 1250°F (675°C) minimum OR Anneal at 1650°F (900°C) |
| Soaking Time | Per thickness |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good - PWHT recommended |
| Electrode Type | E 9018-B 3 |
| Preheating | 300-600°F (150-315°C) |
| Interpass Temperature | 600°F (315°C) max |
| Heat Input | Controlled |
| Post-weld Heat Treatment | 1250°F (675°C) minimum |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - H2S environments, high temperature |
| Applications | High-temperature service up to 649°C (1200°F); Hydrogen service applications; Hydrocracking and hydrotreating units; Steam piping systems; Pressure vessels for elevated temperature |
| Standards | ASTM A182, ASME SA-182, NACE MR0175/ISO 15156 |
| Cost Level | Medium |
| Structure | Ferritic-Pearlitic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 7: ASTM A182 Grade F22V

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - 2.25Cr-1Mo-V |
| Grade | F22V |
| Designation | UNS K31835 |
| CHEMICAL COMPOSITION |  |
| Composition | 2.25% Cr, 1% Mo, 0.25% V |
| Chromium (Cr) | 2.00-2.50% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.87-1.13% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.05-0.15% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 310 MPa min (45 ksi) |
| Elongation | 18% min |
| Hardness | 174-237 HBW |
| HEAT TREATMENT |  |
| Temperature | Normalize & Temper at 1250°F (675°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | 3% Cr, 1% Mo, 0.25% V, Ti |
| Preheating | 300-600°F (150-315°C) |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1250°F (675°C) minimum |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - High temperature |
| Applications | Enhanced creep strength vs F22; High-temperature service; Petrochemical equipment |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Medium |
| Structure | Ferritic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 8: ASTM A182 Grade F23

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - 2.25Cr-1.6W-V-Cb |
| Grade | F23 |
| Designation | UNS K41650 |
| CHEMICAL COMPOSITION |  |
| Composition | 2.25% Cr, 1.6% W, V, Cb |
| Chromium (Cr) | 1.90-2.60% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.04-0.10% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 610 MPa min (88 ksi) |
| Yield Strength | 400 MPa min (58 ksi) |
| Elongation | 20% min |
| Hardness | 220 HBW max |
| HEAT TREATMENT |  |
| Temperature | Normalize at 1900-1975°F (1040-1080°C), Temper at 1350-1470°F (730-800°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good - PWHT mandatory |
| Electrode Type | 2.25% Cr, 1% Mo, 0.25% V |
| Preheating | 300-600°F (150-315°C) |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1350-1470°F (730-800°C) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - High temperature oxidation |
| Applications | Advanced power plants; High-temperature service up to 650°C; Improved creep strength |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | High |
| Structure | Ferritic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 9: ASTM A182 Grade F24

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Low Alloy Steel - 2.25Cr-1Mo-Ti-B |
| Grade | F24 |
| Designation | UNS K30736 |
| CHEMICAL COMPOSITION |  |
| Composition | 2.25% Cr, 1% Mo, Ti, B |
| Chromium (Cr) | 2.20-2.60% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.90-1.10% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.05-0.10% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 585 MPa min (85 ksi) |
| Yield Strength | 415 MPa min (60 ksi) |
| Elongation | 20% min |
| Hardness | 248 HBW max |
| HEAT TREATMENT |  |
| Temperature | Normalize at 1800-1975°F (980-1080°C), Temper at 1350-1470°F (730-800°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good - PWHT mandatory |
| Electrode Type | 2.25% Cr, 1% Mo, 0.25% V |
| Preheating | 300-600°F (150-315°C) |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1350-1470°F (730-800°C) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good |
| Applications | Enhanced creep strength; Power generation; High-temperature piping |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | High |
| Structure | Ferritic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 10: ASTM A182 Grade F91

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Modified 9Cr-1Mo Steel (Advanced Alloy) |
| Grade | F91 |
| Designation | UNS K90901 |
| CHEMICAL COMPOSITION |  |
| Composition | 9% Cr, 1% Mo, V, Nb |
| Chromium (Cr) | 8.00-9.50% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.85-1.05% |
| Nitrogen (N) | 0.030-0.070% |
| Carbon (C) | 0.08-0.12% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 620 MPa min (90 ksi) |
| Yield Strength | 415 MPa min (60 ksi) |
| Elongation | 20% min |
| Hardness | 190-248 HBW |
| HEAT TREATMENT |  |
| Temperature | Normalize at 1900-1975°F (1040-1080°C), Temper at 1350-1470°F (730-800°C) |
| Soaking Time | Per thickness |
| Cooling Method | Air cool or rapid cool |
| WELDING PARAMETERS |  |
| Weldability | Good - PWHT mandatory |
| Electrode Type | 9% Cr, 1% Mo, V, Cb/Nb |
| Preheating | 400-700°F (205-370°C) |
| Interpass Temperature | 700°F (370°C) max |
| Heat Input | Strictly controlled |
| Post-weld Heat Treatment | 1350-1470°F (730-800°C) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Steam oxidation resistance |
| Applications | Ultra-supercritical power plants; High-temperature service up to 650°C (1200°F); Steam headers and main steam piping; Advanced power generation; Cutting-edge material for modern plants |
| Standards | ASTM A182, ASME SA-182, ASME Code Case 1943 |
| Cost Level | High |
| Structure | Tempered Martensitic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 11: ASTM A182 Grade F6a Class 1 (410)

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Martensitic Stainless Steel - 13Cr |
| Grade | F6a |
| Designation | UNS S41000 |
| CHEMICAL COMPOSITION |  |
| Composition | 13% Chromium |
| Chromium (Cr) | 11.5-13.5% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.15% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 485 MPa min (70 ksi) |
| Yield Strength | 275 MPa min (40 ksi) |
| Elongation | 18% min |
| Hardness | 143-207 HBW |
| HEAT TREATMENT |  |
| Temperature | Normalize & Temper at 1325°F (720°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool, then temper |
| WELDING PARAMETERS |  |
| Weldability | Fair - Preheat and PWHT required |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - Mildly corrosive environments |
| Applications | Valve bodies and bonnets; Pump shafts and impellers; Industrial pump components; General engineering parts; Oil and gas equipment |
| Standards | ASTM A182, ASME SA-182, ACI CA-15 |
| Cost Level | Medium |
| Structure | Tempered Martensite |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 12: ASTM A182 Grade F6NM

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Martensitic Stainless Steel - 13Cr-4Ni |
| Grade | F6NM |
| Designation | UNS S41500 |
| CHEMICAL COMPOSITION |  |
| Composition | 13% Cr, 4% Ni |
| Chromium (Cr) | 11.5-14.0% |
| Nickel (Ni) | 3.5-5.5% |
| Molybdenum (Mo) | 0.50-1.00% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.05% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 550 MPa min (80 ksi) |
| Yield Strength | 345 MPa min (50 ksi) |
| Elongation | 18% min |
| Hardness | 220-280 HBW |
| HEAT TREATMENT |  |
| Temperature | Normalize & Temper at 1040-1120°F (560-605°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Enhanced with Ni and Mo |
| Applications | Hydro turbine runners; Marine propellers; Pump casings; Valve components; High-strength corrosion applications |
| Standards | ASTM A182, ASME SA-182, ACI CA-6NM |
| Cost Level | High |
| Structure | Low-carbon Martensite |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 13: ASTM A182 Grade F304

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 |
| Grade | F304 |
| Designation | UNS S30400 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni |
| Chromium (Cr) | 18.0-20.0% |
| Nickel (Ni) | 8.0-11.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.08% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | 143 HBW |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | 30 min per inch of thickness |
| Cooling Method | Rapid quench below 500°F (260°C) in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent - No PWHT needed |
| Electrode Type | E 308-15 or 16 |
| Preheating | Not Required (NR) |
| Interpass Temperature | Not specified |
| Heat Input | Not critical |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - General purpose |
| Applications | Chemical processing equipment; Food and beverage industry; Cryogenic storage tanks (down to -196°C); General-purpose corrosion resistance; Pharmaceutical equipment |
| Standards | ASTM A182, ASME SA-182, ASTM A276 |
| Cost Level | Medium |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 14: ASTM A182 Grade F304L

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 Low Carbon |
| Grade | F304L |
| Designation | UNS S30403 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni (Low Carbon) |
| Chromium (Cr) | 18.0-20.0% |
| Nickel (Ni) | 8.0-13.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 485 MPa min (70 ksi) |
| Yield Strength | 170 MPa min (25 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | 30 min per inch of thickness |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent - Superior to F304 in as-welded condition |
| Electrode Type | E 308L-15 or 16 |
| Preheating | Not Required (NR) |
| Interpass Temperature | Not specified |
| Heat Input | Not critical |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Enhanced weld corrosion resistance |
| Applications | Welded structures (no intergranular corrosion); Cryogenic applications (LNG, liquid nitrogen); Chemical processing; Marine environments; Food processing equipment |
| Standards | ASTM A182, ASME SA-182, EN 1.4306 |
| Cost Level | Medium |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 15: ASTM A182 Grade F316

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-10-2 (Mo Enhanced) |
| Grade | F316 |
| Designation | UNS S31600 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 10% Ni, 2-3% Mo |
| Chromium (Cr) | 16.0-18.0% |
| Nickel (Ni) | 10.0-14.0% |
| Molybdenum (Mo) | 2.00-3.00% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.08% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | 143 HBW |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | 30 min per inch of thickness |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | E 316-15 or 16 |
| Preheating | Not Required (NR) |
| Interpass Temperature | Not specified |
| Heat Input | Not critical |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Enhanced pitting resistance vs F304 |
| Applications | Marine environments (seawater); Chemical processing (aggressive media); Pharmaceutical equipment; Pulp and paper industry; Oil and gas equipment |
| Standards | ASTM A182, ASME SA-182, EN 1.4401 |
| Cost Level | Medium-High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 16: ASTM A182 Grade F316L

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-10-2 Low Carbon |
| Grade | F316L |
| Designation | UNS S31603 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 10% Ni, 2-3% Mo (Low Carbon) |
| Chromium (Cr) | 16.0-18.0% |
| Nickel (Ni) | 10.0-15.0% |
| Molybdenum (Mo) | 2.00-3.00% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 485 MPa min (70 ksi) |
| Yield Strength | 170 MPa min (25 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | 30 min per inch of thickness |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent - Most popular stainless steel |
| Electrode Type | E 316L-15 or 16 |
| Preheating | Not Required (NR) |
| Interpass Temperature | Not specified |
| Heat Input | Not critical |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Best welded corrosion resistance |
| Applications | Marine and offshore structures; Welded equipment in corrosive service; Chemical tankers; Desalination plants; Pharmaceutical clean rooms; Most versatile stainless steel grade |
| Standards | ASTM A182, ASME SA-182, EN 1.4404 |
| Cost Level | Medium-High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 17: ASTM A182 Grade F321

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 Titanium-Stabilized |
| Grade | F321 |
| Designation | UNS S32100 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni, Ti-stabilized |
| Chromium (Cr) | 17.0-19.0% |
| Nickel (Ni) | 9.0-12.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.08% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent - No sensitization |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Prevents intergranular corrosion |
| Applications | High-temperature service (426-870°C); Aircraft exhaust manifolds; Thermal fatigue resistance; Expansion joints; Furnace parts |
| Standards | ASTM A182, ASME SA-182, EN 1.4541 |
| Cost Level | Medium-High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 18: ASTM A182 Grade F347

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 Columbium-Stabilized |
| Grade | F347 |
| Designation | UNS S34700 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni, Cb/Nb-stabilized |
| Chromium (Cr) | 17.0-20.0% |
| Nickel (Ni) | 9.0-13.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.08% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Superior high-temp stability vs F321 |
| Applications | High-temperature applications (better than F321); Petrochemical equipment; Heat exchangers; Pressure vessels for elevated temperature; Superheater tubing |
| Standards | ASTM A182, ASME SA-182, EN 1.4550 |
| Cost Level | Medium-High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 19: ASTM A182 Grade F51 (2205 Duplex)

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Duplex Stainless Steel - 22Cr-5Ni-3Mo-N |
| Grade | F51 |
| Designation | UNS S31803 |
| CHEMICAL COMPOSITION |  |
| Composition | 22% Cr, 5.5% Ni, 3% Mo, N |
| Chromium (Cr) | 21.0-23.0% |
| Nickel (Ni) | 4.5-6.5% |
| Molybdenum (Mo) | 2.5-3.5% |
| Nitrogen (N) | 0.08-0.20% |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 620 MPa min (90 ksi) |
| Yield Strength | 450 MPa min (65 ksi) |
| Elongation | 25% min |
| Hardness | 250 HBW |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1870°F (1020°C) minimum |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Good - Heat input control required |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Chloride SCC resistance |
| Applications | Offshore oil and gas platforms; Subsea pipelines; Pressure vessels (weight savings); Marine and chemical processing; Desalination plants; Cost-effective alternative to 316L with 2× strength |
| Standards | ASTM A182, ASME SA-182, EN 1.4462 |
| Cost Level | High |
| Structure | Duplex (50% Ferrite + 50% Austenite) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 20: ASTM A182 Grade F53 (2507 Super Duplex)

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Super Duplex Stainless Steel - 25Cr-7Ni-4Mo-N |
| Grade | F53 |
| Designation | UNS S32750 |
| CHEMICAL COMPOSITION |  |
| Composition | 25% Cr, 7% Ni, 4% Mo, N |
| Chromium (Cr) | 24.0-26.0% |
| Nickel (Ni) | 6.0-8.0% |
| Molybdenum (Mo) | 3.0-5.0% |
| Nitrogen (N) | 0.24-0.32% |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 800 MPa min (116 ksi) |
| Yield Strength | 550 MPa min (80 ksi) |
| Elongation | 15% min |
| Hardness | 310 HBW max |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Good - Careful heat input control |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Outstanding - Severe chloride environments |
| Applications | Deepwater oil and gas production; Subsea manifolds and trees; High-stress corrosive environments; Offshore platforms (North Sea); Chemical tankers; Extreme service conditions |
| Standards | ASTM A182, ASME SA-182, EN 1.4410, NACE MR0175 |
| Cost Level | Premium |
| Structure | Super Duplex (50% Ferrite + 50% Austenite) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 21: ASTM A182 Grade F20 (Alloy 20)

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Nickel-Iron-Chromium Alloy (Super Austenitic) |
| Grade | F20 |
| Designation | UNS N08020 |
| CHEMICAL COMPOSITION |  |
| Composition | 35% Ni, 20% Cr, 3.5% Cu, 2.5% Mo |
| Chromium (Cr) | 19.0-21.0% |
| Nickel (Ni) | 32.0-38.0% |
| Molybdenum (Mo) | 2.00-3.00% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.07% max |
| Copper (Cu) | 3.0-4.0% |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 725 MPa min (105 ksi) |
| Yield Strength | 345 MPa min (50 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 2050°F (1120°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Outstanding - Sulfuric acid service |
| Applications | Sulfuric acid processing; Aggressive chemical environments; Phosphoric acid plants; Superior pitting and crevice corrosion resistance; Pickling operations |
| Standards | ASTM A182, ASME SA-182, Alloy 20 |
| Cost Level | Premium |
| Structure | Austenitic (Ni-base) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 22: ASTM A182 Grade F44 (254 SMO)

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Super Austenitic Stainless Steel - 6Mo |
| Grade | F44 |
| Designation | UNS S31254 |
| CHEMICAL COMPOSITION |  |
| Composition | 20% Cr, 18% Ni, 6% Mo, N, Cu |
| Chromium (Cr) | 19.5-20.5% |
| Nickel (Ni) | 17.5-18.5% |
| Molybdenum (Mo) | 6.0-6.5% |
| Nitrogen (N) | 0.18-0.22% |
| Carbon (C) | 0.020% max |
| Copper (Cu) | 0.50-1.00% |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 655 MPa min (95 ksi) |
| Yield Strength | 310 MPa min (45 ksi) |
| Elongation | 35% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 2100°F (1150°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Extreme - Seawater and chlorides |
| Applications | Seawater desalination; Oil and gas production; Chemical processing (high chlorides); Offshore platforms; Subsea equipment; Ultimate corrosion resistance |
| Standards | ASTM A182, ASME SA-182, EN 1.4547 |
| Cost Level | Premium |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 23: ASTM A182 Grade F904L

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Super Austenitic Stainless Steel - High Ni-Mo |
| Grade | F904L |
| Designation | UNS N08904 |
| CHEMICAL COMPOSITION |  |
| Composition | 21% Cr, 26% Ni, 4.5% Mo, Cu |
| Chromium (Cr) | 19.0-23.0% |
| Nickel (Ni) | 23.0-28.0% |
| Molybdenum (Mo) | 4.0-5.0% |
| Nitrogen (N) | 0.10% max |
| Carbon (C) | 0.020% max |
| Copper (Cu) | 1.00-2.00% |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 690 MPa min (100 ksi) |
| Yield Strength | 345 MPa min (50 ksi) |
| Elongation | 35% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 2010-2100°F (1100-1150°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Ultimate - Phosphoric/sulfuric acid |
| Applications | Phosphoric acid production; Sulfuric acid handling; Seawater and chloride environments; Chemical processing (most aggressive); Marine scrubber systems; Top-tier corrosion resistance |
| Standards | ASTM A182, ASME SA-182, EN 1.4539 |
| Cost Level | Premium |
| Structure | Austenitic (High Ni) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 24: ASTM A182 Grade F429

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Ferritic Stainless Steel - 15Cr |
| Grade | F429 |
| Designation | UNS S42900 |
| CHEMICAL COMPOSITION |  |
| Composition | 15% Cr |
| Chromium (Cr) | 14.0-16.0% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.12% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 415 MPa min (60 ksi) |
| Yield Strength | 240 MPa min (35 ksi) |
| Elongation | 20% min |
| Hardness | 190 HBW max |
| HEAT TREATMENT |  |
| Temperature | Anneal at 1650°F (900°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Fair |
| Electrode Type | E 430-16 |
| Preheating | 400-700°F (205-370°C) |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - Mildly corrosive |
| Applications | Food processing equipment; Automotive exhaust systems; Heat exchangers |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Low-Medium |
| Structure | Ferritic (BCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 25: ASTM A182 Grade F430

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Ferritic Stainless Steel - 17Cr |
| Grade | F430 |
| Designation | UNS S43000 |
| CHEMICAL COMPOSITION |  |
| Composition | 17% Cr |
| Chromium (Cr) | 16.0-18.0% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.12% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 415 MPa min (60 ksi) |
| Yield Strength | 240 MPa min (35 ksi) |
| Elongation | 20% min |
| Hardness | 190 HBW max |
| HEAT TREATMENT |  |
| Temperature | Anneal - not specified |
| Soaking Time | N/A |
| Cooling Method | Furnace cool |
| WELDING PARAMETERS |  |
| Weldability | Fair |
| Electrode Type | E 430-16 |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - General purpose |
| Applications | Automotive trim; Heat exchangers; General ferritic applications |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Low |
| Structure | Ferritic (BCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 26: ASTM A182 Grade F304H

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 (High Carbon) |
| Grade | F304H |
| Designation | UNS S30409 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni (High Carbon for creep) |
| Chromium (Cr) | 18.0-20.0% |
| Nickel (Ni) | 8.0-11.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.04-0.10% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) |
| Soaking Time | 30 min per inch |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | E 308H-15 or 16 |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent |
| Applications | High-temperature service above 1000°F; Elevated temperature creep resistance; Pressure vessels |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Medium |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 27: ASTM A182 Grade F316H

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-10-2 (High Carbon) |
| Grade | F316H |
| Designation | UNS S31609 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 10% Ni, 2-3% Mo (High Carbon) |
| Chromium (Cr) | 16.0-18.0% |
| Nickel (Ni) | 10.0-14.0% |
| Molybdenum (Mo) | 2.00-3.00% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.04-0.10% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) |
| Soaking Time | 30 min per inch |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | E 316H-15 or 16 |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Enhanced pitting resistance |
| Applications | High-temperature service above 1000°F; Creep resistance applications; Marine and chemical processing |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Medium-High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 28: ASTM A182 Grade F321H

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 Ti-Stabilized (High Carbon) |
| Grade | F321H |
| Designation | UNS S32109 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni, Ti (High Carbon) |
| Chromium (Cr) | 17.0-19.0% |
| Nickel (Ni) | 9.0-12.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.04-0.10% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | E 321-15 or 16 |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Prevents sensitization |
| Applications | High-temperature service (better creep than F321); Aircraft exhaust systems; Thermal cycling resistance |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Medium-High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 29: ASTM A182 Grade F347H

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 Cb-Stabilized (High Carbon) |
| Grade | F347H |
| Designation | UNS S34709 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni, Cb/Nb (High Carbon) |
| Chromium (Cr) | 17.0-19.0% |
| Nickel (Ni) | 9.0-13.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.04-0.10% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | E 347-15 or 16 |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - High temperature stability |
| Applications | High-temperature service (superior to F321H); Petrochemical equipment; Heat exchangers |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Medium-High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 30: ASTM A182 Grade F348

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 Cb-Stabilized (Low Carbon) |
| Grade | F348 |
| Designation | UNS S34800 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni, Cb/Nb |
| Chromium (Cr) | 17.0-19.0% |
| Nickel (Ni) | 9.0-13.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.08% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent - Nuclear applications |
| Electrode Type | E 347-15 or 16 |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1900°F (1040°C) + water quench (if required) |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent |
| Applications | Nuclear applications (Ta controlled); High-purity chemical processing; Special stabilized applications |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 31: ASTM A182 Grade F310H

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 25Cr-20Ni (High Carbon) |
| Grade | F310H |
| Designation | UNS S31009 |
| CHEMICAL COMPOSITION |  |
| Composition | 25% Cr, 20% Ni (High Carbon) |
| Chromium (Cr) | 24.0-26.0% |
| Nickel (Ni) | 19.0-22.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.04-0.10% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 2020-2100°F (1105-1150°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | E 310-15 or 16 |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1920-2010°F (1050-1100°C) + water quench |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - High temperature oxidation |
| Applications | Extreme high-temperature service (superior creep to F310); Furnace parts and fixtures; Heat treatment equipment |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 32: ASTM A182 Grade F310MoLN

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 25Cr-22Ni-Mo-N |
| Grade | F310MoLN |
| Designation | UNS S31050 |
| CHEMICAL COMPOSITION |  |
| Composition | 25% Cr, 22% Ni, Mo, N |
| Chromium (Cr) | 24.0-26.0% |
| Nickel (Ni) | 21.0-23.0% |
| Molybdenum (Mo) | 2.00-3.00% |
| Nitrogen (N) | 0.10-0.16% |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 540 MPa min (78 ksi) |
| Yield Strength | 255 MPa min (37 ksi) |
| Elongation | 25% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1920-2010°F (1050-1100°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | E 310Mo-15 or 16 |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | 1920-2010°F (1050-1100°C) + water quench |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Outstanding - Enhanced with Mo and N |
| Applications | High-temperature service with corrosion; Petrochemical applications; Advanced heat exchangers |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Premium |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 33: ASTM A182 Grade F XM-11

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 20Cr-6Ni-9Mn |
| Grade | F XM-11 |
| Designation | UNS S21904 |
| CHEMICAL COMPOSITION |  |
| Composition | 20% Cr, 6% Ni, 9% Mn |
| Chromium (Cr) | 19.0-21.5% |
| Nickel (Ni) | 5.5-7.5% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | 0.15-0.40% |
| Carbon (C) | 0.040% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 620 MPa min (90 ksi) |
| Yield Strength | 345 MPa min (50 ksi) |
| Elongation | 45% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | XM-11W |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Nickel-conserving grade |
| Applications | Nickel-conserving applications; High strength austenitic; Cryogenic service |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Medium |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 34: ASTM A182 Grade F XM-19

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 22Cr-13Ni-5Mn-2Mo-N |
| Grade | F XM-19 |
| Designation | UNS S20910 |
| CHEMICAL COMPOSITION |  |
| Composition | 22% Cr, 13% Ni, 5% Mn, 2% Mo, N |
| Chromium (Cr) | 20.5-23.5% |
| Nickel (Ni) | 11.5-13.5% |
| Molybdenum (Mo) | 1.50-3.00% |
| Nitrogen (N) | 0.20-0.40% |
| Carbon (C) | 0.06% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 690 MPa min (100 ksi) |
| Yield Strength | 380 MPa min (55 ksi) |
| Elongation | 35% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1700-1850°F (925-1010°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | XM-19W |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - High strength |
| Applications | High strength cryogenic applications; LNG storage; Space applications |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 35: ASTM A182 Grade F50

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Ferritic-Austenitic Stainless Steel - 25Cr-6Ni |
| Grade | F50 |
| Designation | UNS S31200 |
| CHEMICAL COMPOSITION |  |
| Composition | 25% Cr, 6% Ni |
| Chromium (Cr) | 24.0-26.0% |
| Nickel (Ni) | 5.5-6.5% |
| Molybdenum (Mo) | 1.20-2.00% |
| Nitrogen (N) | 0.14-0.20% |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 690 MPa min (100-130 ksi) |
| Yield Strength | 450 MPa min (65 ksi) |
| Elongation | 25% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1925°F (1050°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | 25% Cr, 6% Ni, 1.7% Mo |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Chloride environments |
| Applications | Marine environments; Chemical processing; Duplex stainless applications |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | High |
| Structure | Ferritic-Austenitic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 36: ASTM A182 Grade F52

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Ferritic-Austenitic Stainless Steel - 26Cr-3.5Mo-N |
| Grade | F52 |
| Designation | UNS S32950 |
| CHEMICAL COMPOSITION |  |
| Composition | 26% Cr, 3.5% Mo, 1.6% Mn, N |
| Chromium (Cr) | 26.0-29.0% |
| Nickel (Ni) | 3.5-5.2% |
| Molybdenum (Mo) | 1.00-2.50% |
| Nitrogen (N) | 0.15-0.35% |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 690 MPa min (100-130 ksi) |
| Yield Strength | 450 MPa min (65 ksi) |
| Elongation | 25% min |
| Hardness | 310 HBW max |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | 26% Cr, 3.5% Mo, 1.6% Mn, N |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Outstanding - Severe chloride |
| Applications | Offshore oil and gas; Seawater systems; High-strength duplex |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | High |
| Structure | Ferritic-Austenitic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 37: ASTM A182 Grade F55

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Super Duplex Stainless Steel - 25Cr-7Ni-3.5Mo-W-Cu-N |
| Grade | F55 |
| Designation | UNS S32760 |
| CHEMICAL COMPOSITION |  |
| Composition | 25% Cr, 7% Ni, 3.5% Mo, 0.5-1.0% W, 0.5-1.0% Cu, N |
| Chromium (Cr) | 24.0-26.0% |
| Nickel (Ni) | 6.0-8.0% |
| Molybdenum (Mo) | 3.0-4.0% |
| Nitrogen (N) | 0.20-0.30% |
| Carbon (C) | 0.030% max |
| Copper (Cu) | 0.50-1.00% |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 750 MPa min (109-130 ksi) |
| Yield Strength | 550 MPa min (80 ksi) |
| Elongation | 15% min |
| Hardness | 310 HBW max |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1975-2050°F (1080-1120°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Good - Careful heat input |
| Electrode Type | 25% Cr, 7% Ni, 3.5% Mo |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Ultimate - Most severe chloride |
| Applications | Subsea oil and gas production; Extreme marine environments; Ultimate duplex performance |
| Standards | ASTM A182, ASME SA-182, NACE MR0175 |
| Cost Level | Premium |
| Structure | Super Duplex |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 38: ASTM A182 Grade F60

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Duplex Stainless Steel - 22Cr-5.5Ni-3Mo-N |
| Grade | F60 |
| Designation | UNS S32205 |
| CHEMICAL COMPOSITION |  |
| Composition | 22% Cr, 5.5% Ni, 3% Mo, N |
| Chromium (Cr) | 22.0-23.0% |
| Nickel (Ni) | 4.5-6.5% |
| Molybdenum (Mo) | 3.0-3.5% |
| Nitrogen (N) | 0.14-0.20% |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 620 MPa min (90-130 ksi) |
| Yield Strength | 450 MPa min (65 ksi) |
| Elongation | 25% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1870°F (1020°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Good |
| Electrode Type | 22% Cr, 5.5% Ni, 3% Mo |
| Preheating | NR |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Same as F51/2205 |
| Applications | Offshore platforms; Chemical processing; Marine environments |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | High |
| Structure | Duplex |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 39: ASTM A182 Grade F310

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 25Cr-20Ni |
| Grade | F310 |
| Designation | UNS S31000 |
| CHEMICAL COMPOSITION |  |
| Composition | 25% Cr, 20% Ni |
| Chromium (Cr) | 24.0-26.0% |
| Nickel (Ni) | 19.0-22.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.25% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 2050°F (1120°C) minimum |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - High temperature oxidation |
| Applications | Extreme high-temperature service (up to 1150°C); Heat treatment furnace fixtures; Thermal cycling applications; Oxidizing atmospheres; Best heat resistance of common stainless steels |
| Standards | ASTM A182, ASME SA-182, EN 1.4845 |
| Cost Level | High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 40: ASTM A182 Grade F317L

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-11-3.5 (High Mo) |
| Grade | F317L |
| Designation | UNS S31703 |
| CHEMICAL COMPOSITION |  |
| Composition | 19% Cr, 13% Ni, 3.5% Mo (Low C) |
| Chromium (Cr) | 18.0-20.0% |
| Nickel (Ni) | 11.0-15.0% |
| Molybdenum (Mo) | 3.0-4.0% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 485 MPa min (70 ksi) |
| Yield Strength | 170 MPa min (25 ksi) |
| Elongation | 30% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Superior pitting/crevice resistance |
| Applications | Chemical processing (acidic chlorides); Pulp and paper bleaching; Marine environments; Better corrosion resistance than F316L; Pharmaceutical equipment |
| Standards | ASTM A182, ASME SA-182, EN 1.4438 |
| Cost Level | High |
| Structure | Austenitic (FCC) |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

Material 41: ASTM A182 Grade F92

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Advanced 9Cr-1.8W-V-Nb Steel |
| Grade | F92 |
| Designation | UNS K92460 |
| CHEMICAL COMPOSITION |  |
| Composition | 9% Cr, 1.8% W, V, Nb |
| Chromium (Cr) | 8.50-9.50% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | 0.30-0.60% |
| Nitrogen (N) | 0.030-0.070% |
| Carbon (C) | 0.07-0.13% |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 655 MPa min (95 ksi) |
| Yield Strength | 450 MPa min (65 ksi) |
| Elongation | 20% min |
| Hardness | 248 HBW max |
| HEAT TREATMENT |  |
| Temperature | Normalize at 1900-1975°F (1040-1080°C), Temper at 1350-1470°F (730-800°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Good - PWHT mandatory |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - Steam oxidation |
| Applications | Advanced ultra-supercritical power plants; High-temperature service up to 650°C (1200°F); Fossil fuel power generation; Next-generation steam systems; Improved creep strength vs F91 |
| Standards | ASTM A182, ASME SA-182, ASME Code Case 2179 |
| Cost Level | Premium |
| Structure | Tempered Martensitic |
| Minimum Temperature | N/A |
| Embrittlement Range | N/A |

## RAW EXTRACTED TEXT

=== A182.PDF ===
ASTM A182/A182M-12a Standard Specification
Standard Specification for Forged or Rolled Alloy and Stainless Steel 
Pipe Flanges, Forged Fittings, and Valves and Parts for High-Temperature Service
This specification covers forged or rolled pipe flanges, forged fittings, and valves 
for use in pressure systems at high temperatures. Materials range from low alloy steels 
to high-performance duplex and super austenitic stainless steels.
TOTAL GRADES COVERED: 44+ materials from ASTM A182/A182M-12a
Categories:
- Low Alloy Steels: F1, F5, F9, F11, F12, F22, F22V, F23, F24, F91, F92 (high temperature service)
- Martensitic Stainless: F6a, F6NM (moderate corrosion + strength)
- Ferritic Stainless: F429, F430 (magnetic stainless)
- Austenitic Stainless: F304, F304L, F304H, F316, F316L, F316H, F321, F321H, F347, F347H, F348, F310, F310H, F310MoLN, F317L, F XM-11, F XM-19 (cryogenic to high temp)
- Duplex Stainless: F50, F51, F52, F53, F55, F60 (high strength + excellent corrosion)
- Super Austenitic: F20, F44, F904L (ultimate corrosion resistance)
EXTRACTED MATERIALS:
MATERIAL 1: ASTM A182 Grade F1
Grade: F1
Designation: UNS K12822
Family: Low Alloy Steel - Carbon-Molybdenum
Chemical Composition:
- Type: C-Mo Steel (0.5% Mo)
- Chromium: Not specified
- Nickel: Varies
- Molybdenum: 0.44-0.65%
- Carbon: 0.28% max
Mechanical Properties:
- Tensile Strength: 485 MPa min (70 ksi)
- Yield Strength: 275 MPa min (40 ksi)
- Elongation: 20% min
- Hardness: 143-192 HBW
Heat Treatment:
- Temperature: Anneal at 1550°F (900°C)
- Cooling: Furnace cool
Service Properties:
- Corrosion Resistance: Moderate
- Weldability: Good with preheat
- Microstructure: Ferritic
- Temperature Range: -29°C to 482°C
Applications:
  • Moderate temperature service up to 482°C (900°F)
  • Pressure vessels
  • Piping systems
Standards: ASTM A182, ASME SA-182
---
MATERIAL 2: ASTM A182 Grade F5
Grade: F5
Designation: UNS K41545
Family: Low Alloy Steel - 5Cr-0.5Mo
Chemical Composition:
- Type: 5% Cr, 0.5% Mo
- Chromium: 4.0-6.0%
- Nickel: Varies
- Molybdenum: 0.44-0.65%
- Carbon: 0.15% max
Mechanical Properties:
- Tensile Strength: 485 MPa min (70 ksi)
- Yield Strength: 275 MPa min (40 ksi)
- Elongation: 20% min
- Hardness: 143-217 HBW
Heat Treatment:
- Temperature: Normalize & Temper at 1150°F (620°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Good - High temperature
- Weldability: Good
- Microstructure: Ferritic
- Temperature Range: -29°C to 593°C
Applications:
  • High-temperature service up to 593°C
  • Hydrogen service
  • Refinery equipment
Standards: ASTM A182, ASME SA-182
---
MATERIAL 3: ASTM A182 Grade F9
Grade: F9
Designation: UNS K90901
Family: Low Alloy Steel - 9Cr-1Mo
Chemical Composition:
- Type: 9% Cr, 1% Mo
- Chromium: 8.00-10.00%
- Nickel: Varies
- Molybdenum: 0.90-1.10%
- Carbon: 0.15% max
Mechanical Properties:
- Tensile Strength: 485 MPa min (70 ksi)
- Yield Strength: 275 MPa min (40 ksi)
- Elongation: 20% min
- Hardness: 187-248 HBW
Heat Treatment:
- Temperature: Normalize & Temper at 1250°F (675°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Excellent - Steam oxidation
- Weldability: Good
- Microstructure: Ferritic
- Temperature Range: -29°C to 593°C
Applications:
  • High-temperature service up to 593°C
  • Steam power generation
  • Petrochemical industry
Standards: ASTM A182, ASME SA-182
---
MATERIAL 4: ASTM A182 Grade F11 Class 1
Grade: F11
Designation: UNS K11597
Family: Low Alloy Steel - 1.25Cr-0.5Mo
Chemical Composition:
- Type: 1.25% Cr, 0.5% Mo (Low Carbon)
- Chromium: 1.00-1.50%
- Nickel: Varies
- Molybdenum: 0.44-0.65%
- Carbon: 0.05-0.15%
Mechanical Properties:
- Tensile Strength: 415 MPa min (60 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 20% min
- Hardness: 121-174 HBW
Heat Treatment:
- Temperature: Normalize & Temper at 1150°F (620°C) minimum
- Cooling: Air cool after normalizing
Service Properties:
- Corrosion Resistance: Moderate - High temperature oxidation resistance
- Weldability: Good - Preheat and PWHT required
- Microstructure: Ferritic + Pearlite
- Temperature Range: -29°C to 593°C
Applications:
  • High-temperature piping up to 593°C (1100°F)
  • Steam systems and headers
  • Pressure vessels
  • Refinery and petrochemical equipment
  • Elevated temperature service
Standards: ASTM A182, ASME SA-182, ASTM A370
---
MATERIAL 5: ASTM A182 Grade F12
Grade: F12
Designation: UNS K11572
Family: Low Alloy Steel - 1Cr-0.5Mo
Chemical Composition:
- Type: 1% Cr, 0.5% Mo
- Chromium: 0.80-1.25%
- Nickel: Varies
- Molybdenum: 0.44-0.65%
- Carbon: 0.05-0.15%
Mechanical Properties:
- Tensile Strength: 415 MPa min (60 ksi)
- Yield Strength: 220 MPa min (32 ksi)
- Elongation: 20% min
- Hardness: 156-207 HBW
Heat Treatment:
- Temperature: Normalize & Temper at 1150°F (620°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Moderate
- Weldability: Good
- Microstructure: Ferritic
- Temperature Range: -29°C to 593°C
Applications:
  • High-temperature piping
  • Pressure vessels
  • Petroleum refining
Standards: ASTM A182, ASME SA-182
---
MATERIAL 6: ASTM A182 Grade F22 Class 1
Grade: F22
Designation: UNS K21590
Family: Low Alloy Steel - 2.25Cr-1Mo
Chemical Composition:
- Type: 2.25% Cr, 1% Mo
- Chromium: 2.00-2.50%
- Nickel: Varies
- Molybdenum: 0.87-1.13%
- Carbon: 0.05-0.15%
Mechanical Properties:
- Tensile Strength: 415 MPa min (60 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 20% min
- Hardness: 170 HBW max
Heat Treatment:
- Temperature: Normalize & Temper at 1250°F (675°C) minimum OR Anneal at 1650°F (900°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Good - H2S environments, high temperature
- Weldability: Good - PWHT recommended
- Microstructure: Ferritic-Pearlitic
- Temperature Range: -29°C to 649°C
Applications:
  • High-temperature service up to 649°C (1200°F)
  • Hydrogen service applications
  • Hydrocracking and hydrotreating units
  • Steam piping systems
  • Pressure vessels for elevated temperature
Standards: ASTM A182, ASME SA-182, NACE MR0175/ISO 15156
---
MATERIAL 7: ASTM A182 Grade F22V
Grade: F22V
Designation: UNS K31835
Family: Low Alloy Steel - 2.25Cr-1Mo-V
Chemical Composition:
- Type: 2.25% Cr, 1% Mo, 0.25% V
- Chromium: 2.00-2.50%
- Nickel: Varies
- Molybdenum: 0.87-1.13%
- Carbon: 0.05-0.15%
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 310 MPa min (45 ksi)
- Elongation: 18% min
- Hardness: 174-237 HBW
Heat Treatment:
- Temperature: Normalize & Temper at 1250°F (675°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Good - High temperature
- Weldability: Good
- Microstructure: Ferritic
- Temperature Range: -29°C to 649°C
Applications:
  • Enhanced creep strength vs F22
  • High-temperature service
  • Petrochemical equipment
Standards: ASTM A182, ASME SA-182
---
MATERIAL 8: ASTM A182 Grade F23
Grade: F23
Designation: UNS K41650
Family: Low Alloy Steel - 2.25Cr-1.6W-V-Cb
Chemical Composition:
- Type: 2.25% Cr, 1.6% W, V, Cb
- Chromium: 1.90-2.60%
- Nickel: Varies
- Carbon: 0.04-0.10%
Mechanical Properties:
- Tensile Strength: 610 MPa min (88 ksi)
- Yield Strength: 400 MPa min (58 ksi)
- Elongation: 20% min
- Hardness: 220 HBW max
Heat Treatment:
- Temperature: Normalize at 1900-1975°F (1040-1080°C), Temper at 1350-1470°F (730-800°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Good - High temperature oxidation
- Weldability: Good - PWHT mandatory
- Microstructure: Ferritic
- Temperature Range: -29°C to 650°C
Applications:
  • Advanced power plants
  • High-temperature service up to 650°C
  • Improved creep strength
Standards: ASTM A182, ASME SA-182
---
MATERIAL 9: ASTM A182 Grade F24
Grade: F24
Designation: UNS K30736
Family: Low Alloy Steel - 2.25Cr-1Mo-Ti-B
Chemical Composition:
- Type: 2.25% Cr, 1% Mo, Ti, B
- Chromium: 2.20-2.60%
- Nickel: Varies
- Molybdenum: 0.90-1.10%
- Carbon: 0.05-0.10%
Mechanical Properties:
- Tensile Strength: 585 MPa min (85 ksi)
- Yield Strength: 415 MPa min (60 ksi)
- Elongation: 20% min
- Hardness: 248 HBW max
Heat Treatment:
- Temperature: Normalize at 1800-1975°F (980-1080°C), Temper at 1350-1470°F (730-800°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Good
- Weldability: Good - PWHT mandatory
- Microstructure: Ferritic
- Temperature Range: -29°C to 649°C
Applications:
  • Enhanced creep strength
  • Power generation
  • High-temperature piping
Standards: ASTM A182, ASME SA-182
---
MATERIAL 10: ASTM A182 Grade F91
Grade: F91
Designation: UNS K90901
Family: Modified 9Cr-1Mo Steel (Advanced Alloy)
Chemical Composition:
- Type: 9% Cr, 1% Mo, V, Nb
- Chromium: 8.00-9.50%
- Nickel: Varies
- Molybdenum: 0.85-1.05%
- Nitrogen: 0.030-0.070%
- Carbon: 0.08-0.12%
Mechanical Properties:
- Tensile Strength: 620 MPa min (90 ksi)
- Yield Strength: 415 MPa min (60 ksi)
- Elongation: 20% min
- Hardness: 190-248 HBW
Heat Treatment:
- Temperature: Normalize at 1900-1975°F (1040-1080°C), Temper at 1350-1470°F (730-800°C)
- Cooling: Air cool or rapid cool
Service Properties:
- Corrosion Resistance: Excellent - Steam oxidation resistance
- Weldability: Good - PWHT mandatory
- Microstructure: Tempered Martensitic
- Temperature Range: -29°C to 650°C
Applications:
  • Ultra-supercritical power plants
  • High-temperature service up to 650°C (1200°F)
  • Steam headers and main steam piping
  • Advanced power generation
  • Cutting-edge material for modern plants
Standards: ASTM A182, ASME SA-182, ASME Code Case 1943
---
MATERIAL 11: ASTM A182 Grade F6a Class 1 (410)
Grade: F6a
Designation: UNS S41000
Family: Martensitic Stainless Steel - 13Cr
Chemical Composition:
- Type: 13% Chromium
- Chromium: 11.5-13.5%
- Nickel: Varies
- Carbon: 0.15% max
Mechanical Properties:
- Tensile Strength: 485 MPa min (70 ksi)
- Yield Strength: 275 MPa min (40 ksi)
- Elongation: 18% min
- Hardness: 143-207 HBW
Heat Treatment:
- Temperature: Normalize & Temper at 1325°F (720°C)
- Cooling: Air cool, then temper
Service Properties:
- Corrosion Resistance: Good - Mildly corrosive environments
- Weldability: Fair - Preheat and PWHT required
- Microstructure: Tempered Martensite
- Temperature Range: -29°C to 427°C
Applications:
  • Valve bodies and bonnets
  • Pump shafts and impellers
  • Industrial pump components
  • General engineering parts
  • Oil and gas equipment
Standards: ASTM A182, ASME SA-182, ACI CA-15
---
MATERIAL 12: ASTM A182 Grade F6NM
Grade: F6NM
Designation: UNS S41500
Family: Martensitic Stainless Steel - 13Cr-4Ni
Chemical Composition:
- Type: 13% Cr, 4% Ni
- Chromium: 11.5-14.0%
- Nickel: 3.5-5.5%
- Molybdenum: 0.50-1.00%
- Carbon: 0.05% max
Mechanical Properties:
- Tensile Strength: 550 MPa min (80 ksi)
- Yield Strength: 345 MPa min (50 ksi)
- Elongation: 18% min
- Hardness: 220-280 HBW
Heat Treatment:
- Temperature: Normalize & Temper at 1040-1120°F (560-605°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Excellent - Enhanced with Ni and Mo
- Weldability: Good
- Microstructure: Low-carbon Martensite
- Temperature Range: -46°C to 315°C
Applications:
  • Hydro turbine runners
  • Marine propellers
  • Pump casings
  • Valve components
  • High-strength corrosion applications
Standards: ASTM A182, ASME SA-182, ACI CA-6NM
---
MATERIAL 13: ASTM A182 Grade F304
Grade: F304
Designation: UNS S30400
Family: Austenitic Stainless Steel - 18-8
Chemical Composition:
- Type: 18% Cr, 8% Ni
- Chromium: 18.0-20.0%
- Nickel: 8.0-11.0%
- Carbon: 0.08% max
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: 143 HBW
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C) minimum
- Cooling: Rapid quench below 500°F (260°C) in water
Service Properties:
- Corrosion Resistance: Excellent - General purpose
- Weldability: Excellent - No PWHT needed
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • Chemical processing equipment
  • Food and beverage industry
  • Cryogenic storage tanks (down to -196°C)
  • General-purpose corrosion resistance
  • Pharmaceutical equipment
Standards: ASTM A182, ASME SA-182, ASTM A276
---
MATERIAL 14: ASTM A182 Grade F304L
Grade: F304L
Designation: UNS S30403
Family: Austenitic Stainless Steel - 18-8 Low Carbon
Chemical Composition:
- Type: 18% Cr, 8% Ni (Low Carbon)
- Chromium: 18.0-20.0%
- Nickel: 8.0-13.0%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 485 MPa min (70 ksi)
- Yield Strength: 170 MPa min (25 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C) minimum
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Enhanced weld corrosion resistance
- Weldability: Excellent - Superior to F304 in as-welded condition
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • Welded structures (no intergranular corrosion)
  • Cryogenic applications (LNG, liquid nitrogen)
  • Chemical processing
  • Marine environments
  • Food processing equipment
Standards: ASTM A182, ASME SA-182, EN 1.4306
---
MATERIAL 15: ASTM A182 Grade F316
Grade: F316
Designation: UNS S31600
Family: Austenitic Stainless Steel - 18-10-2 (Mo Enhanced)
Chemical Composition:
- Type: 18% Cr, 10% Ni, 2-3% Mo
- Chromium: 16.0-18.0%
- Nickel: 10.0-14.0%
- Molybdenum: 2.00-3.00%
- Carbon: 0.08% max
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: 143 HBW
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C) minimum
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Enhanced pitting resistance vs F304
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • Marine environments (seawater)
  • Chemical processing (aggressive media)
  • Pharmaceutical equipment
  • Pulp and paper industry
  • Oil and gas equipment
Standards: ASTM A182, ASME SA-182, EN 1.4401
---
MATERIAL 16: ASTM A182 Grade F316L
Grade: F316L
Designation: UNS S31603
Family: Austenitic Stainless Steel - 18-10-2 Low Carbon
Chemical Composition:
- Type: 18% Cr, 10% Ni, 2-3% Mo (Low Carbon)
- Chromium: 16.0-18.0%
- Nickel: 10.0-15.0%
- Molybdenum: 2.00-3.00%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 485 MPa min (70 ksi)
- Yield Strength: 170 MPa min (25 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C) minimum
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Best welded corrosion resistance
- Weldability: Excellent - Most popular stainless steel
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • Marine and offshore structures
  • Welded equipment in corrosive service
  • Chemical tankers
  • Desalination plants
  • Pharmaceutical clean rooms
  • Most versatile stainless steel grade
Standards: ASTM A182, ASME SA-182, EN 1.4404
---
MATERIAL 17: ASTM A182 Grade F321
Grade: F321
Designation: UNS S32100
Family: Austenitic Stainless Steel - 18-8 Titanium-Stabilized
Chemical Composition:
- Type: 18% Cr, 8% Ni, Ti-stabilized
- Chromium: 17.0-19.0%
- Nickel: 9.0-12.0%
- Carbon: 0.08% max
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C) minimum
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Prevents intergranular corrosion
- Weldability: Excellent - No sensitization
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • High-temperature service (426-870°C)
  • Aircraft exhaust manifolds
  • Thermal fatigue resistance
  • Expansion joints
  • Furnace parts
Standards: ASTM A182, ASME SA-182, EN 1.4541
---
MATERIAL 18: ASTM A182 Grade F347
Grade: F347
Designation: UNS S34700
Family: Austenitic Stainless Steel - 18-8 Columbium-Stabilized
Chemical Composition:
- Type: 18% Cr, 8% Ni, Cb/Nb-stabilized
- Chromium: 17.0-20.0%
- Nickel: 9.0-13.0%
- Carbon: 0.08% max
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C) minimum
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Superior high-temp stability vs F321
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • High-temperature applications (better than F321)
  • Petrochemical equipment
  • Heat exchangers
  • Pressure vessels for elevated temperature
  • Superheater tubing
Standards: ASTM A182, ASME SA-182, EN 1.4550
---
MATERIAL 19: ASTM A182 Grade F51 (2205 Duplex)
Grade: F51
Designation: UNS S31803
Family: Duplex Stainless Steel - 22Cr-5Ni-3Mo-N
Chemical Composition:
- Type: 22% Cr, 5.5% Ni, 3% Mo, N
- Chromium: 21.0-23.0%
- Nickel: 4.5-6.5%
- Molybdenum: 2.5-3.5%
- Nitrogen: 0.08-0.20%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 620 MPa min (90 ksi)
- Yield Strength: 450 MPa min (65 ksi)
- Elongation: 25% min
- Hardness: 250 HBW
Heat Treatment:
- Temperature: Solution anneal at 1870°F (1020°C) minimum
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Chloride SCC resistance
- Weldability: Good - Heat input control required
- Microstructure: Duplex (50% Ferrite + 50% Austenite)
- Temperature Range: -50°C to 315°C
Applications:
  • Offshore oil and gas platforms
  • Subsea pipelines
  • Pressure vessels (weight savings)
  • Marine and chemical processing
  • Desalination plants
  • Cost-effective alternative to 316L with 2× strength
Standards: ASTM A182, ASME SA-182, EN 1.4462
---
MATERIAL 20: ASTM A182 Grade F53 (2507 Super Duplex)
Grade: F53
Designation: UNS S32750
Family: Super Duplex Stainless Steel - 25Cr-7Ni-4Mo-N
Chemical Composition:
- Type: 25% Cr, 7% Ni, 4% Mo, N
- Chromium: 24.0-26.0%
- Nickel: 6.0-8.0%
- Molybdenum: 3.0-5.0%
- Nitrogen: 0.24-0.32%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 800 MPa min (116 ksi)
- Yield Strength: 550 MPa min (80 ksi)
- Elongation: 15% min
- Hardness: 310 HBW max
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C) minimum
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Outstanding - Severe chloride environments
- Weldability: Good - Careful heat input control
- Microstructure: Super Duplex (50% Ferrite + 50% Austenite)
- Temperature Range: -50°C to 250°C
Applications:
  • Deepwater oil and gas production
  • Subsea manifolds and trees
  • High-stress corrosive environments
  • Offshore platforms (North Sea)
  • Chemical tankers
  • Extreme service conditions
Standards: ASTM A182, ASME SA-182, EN 1.4410, NACE MR0175
---
MATERIAL 21: ASTM A182 Grade F20 (Alloy 20)
Grade: F20
Designation: UNS N08020
Family: Nickel-Iron-Chromium Alloy (Super Austenitic)
Chemical Composition:
- Type: 35% Ni, 20% Cr, 3.5% Cu, 2.5% Mo
- Chromium: 19.0-21.0%
- Nickel: 32.0-38.0%
- Molybdenum: 2.00-3.00%
- Carbon: 0.07% max
Mechanical Properties:
- Tensile Strength: 725 MPa min (105 ksi)
- Yield Strength: 345 MPa min (50 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 2050°F (1120°C)
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Outstanding - Sulfuric acid service
- Weldability: Good
- Microstructure: Austenitic (Ni-base)
- Temperature Range: -29°C to 538°C
Applications:
  • Sulfuric acid processing
  • Aggressive chemical environments
  • Phosphoric acid plants
  • Superior pitting and crevice corrosion resistance
  • Pickling operations
Standards: ASTM A182, ASME SA-182, Alloy 20
---
MATERIAL 22: ASTM A182 Grade F44 (254 SMO)
Grade: F44
Designation: UNS S31254
Family: Super Austenitic Stainless Steel - 6Mo
Chemical Composition:
- Type: 20% Cr, 18% Ni, 6% Mo, N, Cu
- Chromium: 19.5-20.5%
- Nickel: 17.5-18.5%
- Molybdenum: 6.0-6.5%
- Nitrogen: 0.18-0.22%
- Carbon: 0.020% max
Mechanical Properties:
- Tensile Strength: 655 MPa min (95 ksi)
- Yield Strength: 310 MPa min (45 ksi)
- Elongation: 35% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 2100°F (1150°C)
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Extreme - Seawater and chlorides
- Weldability: Good
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 400°C
Applications:
  • Seawater desalination
  • Oil and gas production
  • Chemical processing (high chlorides)
  • Offshore platforms
  • Subsea equipment
  • Ultimate corrosion resistance
Standards: ASTM A182, ASME SA-182, EN 1.4547
---
MATERIAL 23: ASTM A182 Grade F904L
Grade: F904L
Designation: UNS N08904
Family: Super Austenitic Stainless Steel - High Ni-Mo
Chemical Composition:
- Type: 21% Cr, 26% Ni, 4.5% Mo, Cu
- Chromium: 19.0-23.0%
- Nickel: 23.0-28.0%
- Molybdenum: 4.0-5.0%
- Nitrogen: 0.10% max
- Carbon: 0.020% max
Mechanical Properties:
- Tensile Strength: 690 MPa min (100 ksi)
- Yield Strength: 345 MPa min (50 ksi)
- Elongation: 35% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 2010-2100°F (1100-1150°C)
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Ultimate - Phosphoric/sulfuric acid
- Weldability: Excellent
- Microstructure: Austenitic (High Ni)
- Temperature Range: -196°C to 400°C
Applications:
  • Phosphoric acid production
  • Sulfuric acid handling
  • Seawater and chloride environments
  • Chemical processing (most aggressive)
  • Marine scrubber systems
  • Top-tier corrosion resistance
Standards: ASTM A182, ASME SA-182, EN 1.4539
---
MATERIAL 24: ASTM A182 Grade F429
Grade: F429
Designation: UNS S42900
Family: Ferritic Stainless Steel - 15Cr
Chemical Composition:
- Type: 15% Cr
- Chromium: 14.0-16.0%
- Nickel: Varies
- Carbon: 0.12% max
Mechanical Properties:
- Tensile Strength: 415 MPa min (60 ksi)
- Yield Strength: 240 MPa min (35 ksi)
- Elongation: 20% min
- Hardness: 190 HBW max
Heat Treatment:
- Temperature: Anneal at 1650°F (900°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Good - Mildly corrosive
- Weldability: Fair
- Microstructure: Ferritic (BCC)
- Temperature Range: -29°C to 427°C
Applications:
  • Food processing equipment
  • Automotive exhaust systems
  • Heat exchangers
Standards: ASTM A182, ASME SA-182
---
MATERIAL 25: ASTM A182 Grade F430
Grade: F430
Designation: UNS S43000
Family: Ferritic Stainless Steel - 17Cr
Chemical Composition:
- Type: 17% Cr
- Chromium: 16.0-18.0%
- Nickel: Varies
- Carbon: 0.12% max
Mechanical Properties:
- Tensile Strength: 415 MPa min (60 ksi)
- Yield Strength: 240 MPa min (35 ksi)
- Elongation: 20% min
- Hardness: 190 HBW max
Heat Treatment:
- Temperature: Anneal - not specified
- Cooling: Furnace cool
Service Properties:
- Corrosion Resistance: Good - General purpose
- Weldability: Fair
- Microstructure: Ferritic (BCC)
- Temperature Range: -29°C to 427°C
Applications:
  • Automotive trim
  • Heat exchangers
  • General ferritic applications
Standards: ASTM A182, ASME SA-182
---
MATERIAL 26: ASTM A182 Grade F304H
Grade: F304H
Designation: UNS S30409
Family: Austenitic Stainless Steel - 18-8 (High Carbon)
Chemical Composition:
- Type: 18% Cr, 8% Ni (High Carbon for creep)
- Chromium: 18.0-20.0%
- Nickel: 8.0-11.0%
- Carbon: 0.04-0.10%
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • High-temperature service above 1000°F
  • Elevated temperature creep resistance
  • Pressure vessels
Standards: ASTM A182, ASME SA-182
---
MATERIAL 27: ASTM A182 Grade F316H
Grade: F316H
Designation: UNS S31609
Family: Austenitic Stainless Steel - 18-10-2 (High Carbon)
Chemical Composition:
- Type: 18% Cr, 10% Ni, 2-3% Mo (High Carbon)
- Chromium: 16.0-18.0%
- Nickel: 10.0-14.0%
- Molybdenum: 2.00-3.00%
- Carbon: 0.04-0.10%
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Enhanced pitting resistance
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • High-temperature service above 1000°F
  • Creep resistance applications
  • Marine and chemical processing
Standards: ASTM A182, ASME SA-182
---
MATERIAL 28: ASTM A182 Grade F321H
Grade: F321H
Designation: UNS S32109
Family: Austenitic Stainless Steel - 18-8 Ti-Stabilized (High Carbon)
Chemical Composition:
- Type: 18% Cr, 8% Ni, Ti (High Carbon)
- Chromium: 17.0-19.0%
- Nickel: 9.0-12.0%
- Carbon: 0.04-0.10%
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Prevents sensitization
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • High-temperature service (better creep than F321)
  • Aircraft exhaust systems
  • Thermal cycling resistance
Standards: ASTM A182, ASME SA-182
---
MATERIAL 29: ASTM A182 Grade F347H
Grade: F347H
Designation: UNS S34709
Family: Austenitic Stainless Steel - 18-8 Cb-Stabilized (High Carbon)
Chemical Composition:
- Type: 18% Cr, 8% Ni, Cb/Nb (High Carbon)
- Chromium: 17.0-19.0%
- Nickel: 9.0-13.0%
- Carbon: 0.04-0.10%
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - High temperature stability
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • High-temperature service (superior to F321H)
  • Petrochemical equipment
  • Heat exchangers
Standards: ASTM A182, ASME SA-182
---
MATERIAL 30: ASTM A182 Grade F348
Grade: F348
Designation: UNS S34800
Family: Austenitic Stainless Steel - 18-8 Cb-Stabilized (Low Carbon)
Chemical Composition:
- Type: 18% Cr, 8% Ni, Cb/Nb
- Chromium: 17.0-19.0%
- Nickel: 9.0-13.0%
- Carbon: 0.08% max
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent
- Weldability: Excellent - Nuclear applications
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • Nuclear applications (Ta controlled)
  • High-purity chemical processing
  • Special stabilized applications
Standards: ASTM A182, ASME SA-182
---
MATERIAL 31: ASTM A182 Grade F310H
Grade: F310H
Designation: UNS S31009
Family: Austenitic Stainless Steel - 25Cr-20Ni (High Carbon)
Chemical Composition:
- Type: 25% Cr, 20% Ni (High Carbon)
- Chromium: 24.0-26.0%
- Nickel: 19.0-22.0%
- Carbon: 0.04-0.10%
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 2020-2100°F (1105-1150°C)
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Excellent - High temperature oxidation
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 1150°C
Applications:
  • Extreme high-temperature service (superior creep to F310)
  • Furnace parts and fixtures
  • Heat treatment equipment
Standards: ASTM A182, ASME SA-182
---
MATERIAL 32: ASTM A182 Grade F310MoLN
Grade: F310MoLN
Designation: UNS S31050
Family: Austenitic Stainless Steel - 25Cr-22Ni-Mo-N
Chemical Composition:
- Type: 25% Cr, 22% Ni, Mo, N
- Chromium: 24.0-26.0%
- Nickel: 21.0-23.0%
- Molybdenum: 2.00-3.00%
- Nitrogen: 0.10-0.16%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 540 MPa min (78 ksi)
- Yield Strength: 255 MPa min (37 ksi)
- Elongation: 25% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1920-2010°F (1050-1100°C)
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Outstanding - Enhanced with Mo and N
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 1100°C
Applications:
  • High-temperature service with corrosion
  • Petrochemical applications
  • Advanced heat exchangers
Standards: ASTM A182, ASME SA-182
---
MATERIAL 33: ASTM A182 Grade F XM-11
Grade: F XM-11
Designation: UNS S21904
Family: Austenitic Stainless Steel - 20Cr-6Ni-9Mn
Chemical Composition:
- Type: 20% Cr, 6% Ni, 9% Mn
- Chromium: 19.0-21.5%
- Nickel: 5.5-7.5%
- Nitrogen: 0.15-0.40%
- Carbon: 0.040% max
Mechanical Properties:
- Tensile Strength: 620 MPa min (90 ksi)
- Yield Strength: 345 MPa min (50 ksi)
- Elongation: 45% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C)
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Excellent - Nickel-conserving grade
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • Nickel-conserving applications
  • High strength austenitic
  • Cryogenic service
Standards: ASTM A182, ASME SA-182
---
MATERIAL 34: ASTM A182 Grade F XM-19
Grade: F XM-19
Designation: UNS S20910
Family: Austenitic Stainless Steel - 22Cr-13Ni-5Mn-2Mo-N
Chemical Composition:
- Type: 22% Cr, 13% Ni, 5% Mn, 2% Mo, N
- Chromium: 20.5-23.5%
- Nickel: 11.5-13.5%
- Molybdenum: 1.50-3.00%
- Nitrogen: 0.20-0.40%
- Carbon: 0.06% max
Mechanical Properties:
- Tensile Strength: 690 MPa min (100 ksi)
- Yield Strength: 380 MPa min (55 ksi)
- Elongation: 35% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1700-1850°F (925-1010°C)
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Excellent - High strength
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • High strength cryogenic applications
  • LNG storage
  • Space applications
Standards: ASTM A182, ASME SA-182
---
MATERIAL 35: ASTM A182 Grade F50
Grade: F50
Designation: UNS S31200
Family: Ferritic-Austenitic Stainless Steel - 25Cr-6Ni
Chemical Composition:
- Type: 25% Cr, 6% Ni
- Chromium: 24.0-26.0%
- Nickel: 5.5-6.5%
- Molybdenum: 1.20-2.00%
- Nitrogen: 0.14-0.20%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 690 MPa min (100-130 ksi)
- Yield Strength: 450 MPa min (65 ksi)
- Elongation: 25% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1925°F (1050°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Chloride environments
- Weldability: Good
- Microstructure: Ferritic-Austenitic
- Temperature Range: -50°C to 315°C
Applications:
  • Marine environments
  • Chemical processing
  • Duplex stainless applications
Standards: ASTM A182, ASME SA-182
---
MATERIAL 36: ASTM A182 Grade F52
Grade: F52
Designation: UNS S32950
Family: Ferritic-Austenitic Stainless Steel - 26Cr-3.5Mo-N
Chemical Composition:
- Type: 26% Cr, 3.5% Mo, 1.6% Mn, N
- Chromium: 26.0-29.0%
- Nickel: 3.5-5.2%
- Molybdenum: 1.00-2.50%
- Nitrogen: 0.15-0.35%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 690 MPa min (100-130 ksi)
- Yield Strength: 450 MPa min (65 ksi)
- Elongation: 25% min
- Hardness: 310 HBW max
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Outstanding - Severe chloride
- Weldability: Good
- Microstructure: Ferritic-Austenitic
- Temperature Range: -50°C to 315°C
Applications:
  • Offshore oil and gas
  • Seawater systems
  • High-strength duplex
Standards: ASTM A182, ASME SA-182
---
MATERIAL 37: ASTM A182 Grade F55
Grade: F55
Designation: UNS S32760
Family: Super Duplex Stainless Steel - 25Cr-7Ni-3.5Mo-W-Cu-N
Chemical Composition:
- Type: 25% Cr, 7% Ni, 3.5% Mo, 0.5-1.0% W, 0.5-1.0% Cu, N
- Chromium: 24.0-26.0%
- Nickel: 6.0-8.0%
- Molybdenum: 3.0-4.0%
- Nitrogen: 0.20-0.30%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 750 MPa min (109-130 ksi)
- Yield Strength: 550 MPa min (80 ksi)
- Elongation: 15% min
- Hardness: 310 HBW max
Heat Treatment:
- Temperature: Solution anneal at 1975-2050°F (1080-1120°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Ultimate - Most severe chloride
- Weldability: Good - Careful heat input
- Microstructure: Super Duplex
- Temperature Range: -50°C to 250°C
Applications:
  • Subsea oil and gas production
  • Extreme marine environments
  • Ultimate duplex performance
Standards: ASTM A182, ASME SA-182, NACE MR0175
---
MATERIAL 38: ASTM A182 Grade F60
Grade: F60
Designation: UNS S32205
Family: Duplex Stainless Steel - 22Cr-5.5Ni-3Mo-N
Chemical Composition:
- Type: 22% Cr, 5.5% Ni, 3% Mo, N
- Chromium: 22.0-23.0%
- Nickel: 4.5-6.5%
- Molybdenum: 3.0-3.5%
- Nitrogen: 0.14-0.20%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 620 MPa min (90-130 ksi)
- Yield Strength: 450 MPa min (65 ksi)
- Elongation: 25% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1870°F (1020°C)
- Cooling: Rapid quench below 500°F in water
Service Properties:
- Corrosion Resistance: Excellent - Same as F51/2205
- Weldability: Good
- Microstructure: Duplex
- Temperature Range: -50°C to 315°C
Applications:
  • Offshore platforms
  • Chemical processing
  • Marine environments
Standards: ASTM A182, ASME SA-182
---
MATERIAL 39: ASTM A182 Grade F310
Grade: F310
Designation: UNS S31000
Family: Austenitic Stainless Steel - 25Cr-20Ni
Chemical Composition:
- Type: 25% Cr, 20% Ni
- Chromium: 24.0-26.0%
- Nickel: 19.0-22.0%
- Carbon: 0.25% max
Mechanical Properties:
- Tensile Strength: 515 MPa min (75 ksi)
- Yield Strength: 205 MPa min (30 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 2050°F (1120°C) minimum
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Excellent - High temperature oxidation
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 1150°C
Applications:
  • Extreme high-temperature service (up to 1150°C)
  • Heat treatment furnace fixtures
  • Thermal cycling applications
  • Oxidizing atmospheres
  • Best heat resistance of common stainless steels
Standards: ASTM A182, ASME SA-182, EN 1.4845
---
MATERIAL 40: ASTM A182 Grade F317L
Grade: F317L
Designation: UNS S31703
Family: Austenitic Stainless Steel - 18-11-3.5 (High Mo)
Chemical Composition:
- Type: 19% Cr, 13% Ni, 3.5% Mo (Low C)
- Chromium: 18.0-20.0%
- Nickel: 11.0-15.0%
- Molybdenum: 3.0-4.0%
- Carbon: 0.030% max
Mechanical Properties:
- Tensile Strength: 485 MPa min (70 ksi)
- Yield Strength: 170 MPa min (25 ksi)
- Elongation: 30% min
- Hardness: Not specified
Heat Treatment:
- Temperature: Solution anneal at 1900°F (1040°C) minimum
- Cooling: Rapid quench
Service Properties:
- Corrosion Resistance: Excellent - Superior pitting/crevice resistance
- Weldability: Excellent
- Microstructure: Austenitic (FCC)
- Temperature Range: -196°C to 870°C
Applications:
  • Chemical processing (acidic chlorides)
  • Pulp and paper bleaching
  • Marine environments
  • Better corrosion resistance than F316L
  • Pharmaceutical equipment
Standards: ASTM A182, ASME SA-182, EN 1.4438
---
MATERIAL 41: ASTM A182 Grade F92
Grade: F92
Designation: UNS K92460
Family: Advanced 9Cr-1.8W-V-Nb Steel
Chemical Composition:
- Type: 9% Cr, 1.8% W, V, Nb
- Chromium: 8.50-9.50%
- Nickel: Varies
- Molybdenum: 0.30-0.60%
- Nitrogen: 0.030-0.070%
- Carbon: 0.07-0.13%
Mechanical Properties:
- Tensile Strength: 655 MPa min (95 ksi)
- Yield Strength: 450 MPa min (65 ksi)
- Elongation: 20% min
- Hardness: 248 HBW max
Heat Treatment:
- Temperature: Normalize at 1900-1975°F (1040-1080°C), Temper at 1350-1470°F (730-800°C)
- Cooling: Air cool
Service Properties:
- Corrosion Resistance: Good - Steam oxidation
- Weldability: Good - PWHT mandatory
- Microstructure: Tempered Martensitic
- Temperature Range: -29°C to 650°C
Applications:
  • Advanced ultra-supercritical power plants
  • High-temperature service up to 650°C (1200°F)
  • Fossil fuel power generation
  • Next-generation steam systems
  • Improved creep strength vs F91
Standards: ASTM A182, ASME SA-182, ASME Code Case 2179
---
CRITICAL TEMPERATURE LIMITS:
- Low Alloy Steels (F11, F22, F91, F92): -29°C to 593-650°C
- Martensitic Stainless (F6a, F6NM): -29°C to 315-427°C
- Austenitic Stainless (F304/L, F316/L, F321, F347, F310): -196°C to 870-1150°C
- Duplex Stainless (F51, F53): -50°C to 250-315°C
- Super Austenitic (F20, F44, F904L): -196°C to 400-538°C
CRYOGENIC SERVICE: ONLY austenitic grades (F304, F304L, F316, F316L, F321, F347, F310, F317L, F44, F904L) 
are suitable for temperatures below -100°C. Duplex steels FAIL below -50°C due to ferrite embrittlement.
MATERIAL SELECTION GUIDE:
- General Purpose: F304/F304L
- Seawater/Marine: F316L (moderate), F44/F904L (severe)
- High Strength + Corrosion: F51 (duplex 2205), F53 (super duplex 2507)
- High Temperature: F91/F92 (up to 650°C), F310 (up to 1150°C)
- Cryogenic: F304L, F316L, F321, F347 (down to -196°C)
- Ultimate Corrosion: F904L (phosphoric/sulfuric acid, chlorides)