# MATERIAL EXTRACTION REPORT

Generated: 2/2/2026, 5:06:45 PM

Total Materials: 3

Source: Audco India Ltd Technical Bulletin No: 1

## EXTRACTED MATERIALS

Material 1: ASTM A182 Grade F304

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-8 |
| Grade | F304 |
| Designation | UNS S30400 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 8% Ni |
| Chromium (Cr) | 18.0-20.0% |
| Nickel (Ni) | 8.0-11.0% |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.08% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | 143 HBW |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F (260°C) in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent - No PWHT needed |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - General purpose |
| Applications | Chemical processing equipment; Food and beverage industry; Cryogenic storage tanks (down to -196°C); General-purpose corrosion resistance; Pharmaceutical equipment |
| Standards | ASTM A182, ASME SA-182, ASTM A276 |
| Cost Level | Medium |
| Structure | Austenitic (FCC) |
| Minimum Temperature |  |
| Embrittlement Range | N/A |

Material 2: ASTM A182 Grade F316

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 18-10-2 (Mo Enhanced) |
| Grade | F316 |
| Designation | UNS S31600 |
| CHEMICAL COMPOSITION |  |
| Composition | 18% Cr, 10% Ni, 2-3% Mo |
| Chromium (Cr) | 16.0-18.0% |
| Nickel (Ni) | 10.0-14.0% |
| Molybdenum (Mo) | 2.00-3.00% |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.08% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 515 MPa min (75 ksi) |
| Yield Strength | 205 MPa min (30 ksi) |
| Elongation | 30% min |
| Hardness | 143 HBW |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1900°F (1040°C) minimum |
| Soaking Time | N/A |
| Cooling Method | Rapid quench below 500°F in water |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Excellent - Enhanced pitting resistance vs F304 |
| Applications | Marine environments (seawater); Chemical processing (aggressive media); Pharmaceutical equipment; Pulp and paper industry; Oil and gas equipment |
| Standards | ASTM A182, ASME SA-182, EN 1.4401 |
| Cost Level | Medium-High |
| Structure | Austenitic (FCC) |
| Minimum Temperature |  |
| Embrittlement Range | N/A |

Material 3: ASTM A182 Grade F310MoLN

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Austenitic Stainless Steel - 25Cr-22Ni-Mo-N |
| Grade | F310MoLN |
| Designation | UNS S31050 |
| CHEMICAL COMPOSITION |  |
| Composition | 25% Cr, 22% Ni, Mo, N |
| Chromium (Cr) | 24.0-26.0% |
| Nickel (Ni) | 21.0-23.0% |
| Molybdenum (Mo) | 2.00-3.00% |
| Nitrogen (N) | 0.10-0.16% |
| Carbon (C) | 0.030% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 540 MPa min (78 ksi) |
| Yield Strength | 255 MPa min (37 ksi) |
| Elongation | 25% min |
| Hardness | Not specified |
| HEAT TREATMENT |  |
| Temperature | Solution anneal at 1920-2010°F (1050-1100°C) |
| Soaking Time | N/A |
| Cooling Method | Rapid quench |
| WELDING PARAMETERS |  |
| Weldability | Excellent |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Outstanding - Enhanced with Mo and N |
| Applications | High-temperature service with corrosion; Petrochemical applications; Advanced heat exchangers |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Premium |
| Structure | Austenitic (FCC) |
| Minimum Temperature |  |
| Embrittlement Range | N/A |

## RAW EXTRACTED TEXT

1. Austenitic Stainless Steel - 18-8 - Grade: F304
Overall Score: 91
Recommendation: Excellent match - F304 exceeds all requirements with optimal cost-performance ratio
2. Austenitic Stainless Steel - 18-10-2 (Mo Enhanced) - Grade: F316
Overall Score: 91
Recommendation: Excellent match - F316 exceeds all requirements with optimal cost-performance ratio
3. Austenitic Stainless Steel - 25Cr-22Ni-Mo-N - Grade: F310MoLN
Overall Score: 91
Recommendation: Excellent match - F310MoLN exceeds all requirements with optimal cost-performance ratio