# MATERIAL EXTRACTION REPORT

Generated: 2/2/2026, 9:50:38 PM

Total Materials: 2

Source: Audco India Ltd Technical Bulletin No: 1

## EXTRACTED MATERIALS

Material 1: ASTM A182 Grade F429

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Ferritic Stainless Steel - 15Cr |
| Grade | F429 |
| Designation | UNS S42900 |
| CHEMICAL COMPOSITION |  |
| Composition | 15% Cr |
| Chromium (Cr) | 14.0-16.0% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.12% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 415 MPa min (60 ksi) |
| Yield Strength | 240 MPa min (35 ksi) |
| Elongation | 20% min |
| Hardness | 190 HBW max |
| HEAT TREATMENT |  |
| Temperature | Anneal at 1650°F (900°C) |
| Soaking Time | N/A |
| Cooling Method | Air cool |
| WELDING PARAMETERS |  |
| Weldability | Fair |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - Mildly corrosive |
| Applications | Food processing equipment; Automotive exhaust systems; Heat exchangers |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Low-Medium |
| Structure | Ferritic (BCC) |
| Minimum Temperature |  |
| Embrittlement Range | N/A |

Material 2: ASTM A182 Grade F430

| BASIC INFORMATION |  |
| --- | --- |
| Material Family | Ferritic Stainless Steel - 17Cr |
| Grade | F430 |
| Designation | UNS S43000 |
| CHEMICAL COMPOSITION |  |
| Composition | 17% Cr |
| Chromium (Cr) | 16.0-18.0% |
| Nickel (Ni) | N/A |
| Molybdenum (Mo) | N/A |
| Nitrogen (N) | N/A |
| Carbon (C) | 0.12% max |
| Copper (Cu) | N/A |
| MECHANICAL PROPERTIES |  |
| Tensile Strength | 415 MPa min (60 ksi) |
| Yield Strength | 240 MPa min (35 ksi) |
| Elongation | 20% min |
| Hardness | 190 HBW max |
| HEAT TREATMENT |  |
| Temperature | Anneal - not specified |
| Soaking Time | N/A |
| Cooling Method | Furnace cool |
| WELDING PARAMETERS |  |
| Weldability | Fair |
| Electrode Type | N/A |
| Preheating | N/A |
| Interpass Temperature | N/A |
| Heat Input | N/A |
| Post-weld Heat Treatment | N/A |
| ADDITIONAL PROPERTIES |  |
| Corrosion Resistance | Good - General purpose |
| Applications | Automotive trim; Heat exchangers; General ferritic applications |
| Standards | ASTM A182, ASME SA-182 |
| Cost Level | Low |
| Structure | Ferritic (BCC) |
| Minimum Temperature |  |
| Embrittlement Range | N/A |

## RAW EXTRACTED TEXT

1. Ferritic Stainless Steel - 15Cr - Grade: F429
Overall Score: 78
Recommendation: Good option - F429 satisfies most requirements with minor compromises
2. Ferritic Stainless Steel - 17Cr - Grade: F430
Overall Score: 78
Recommendation: Good option - F430 satisfies most requirements with minor compromises